# INTUMAX FR86PVC

Broadview Technologies, Inc’s Intumax FR86PVC is a 75C fire retardant pvc compound.  It is

formulated with our trade marked Intumax™ technology. It has excellent processing, and low smoke characteristics.

TYPICAL PHYSICAL PROPERTIES OF MOLDED SLAB (0.075")

COMPOUND                                TYPICAL VALUES                 TEST METHOD

Specific Gravity			                                 1.59                             	       ASTM D-792

Hardness, Duro. A 				    86 	    		       ASTM D-2240

10 Sec.(+/-3)

Tensile Strength, Psi				    2300			       ASTM D-638

Elongation, %					      320	   		       ASTM D-638

Limiting Oxygen Index %                                                     39.5                                       ASTM D-2863

Recommended Stock Temperature         360F

Colors:  Multiple colors available